Supporting information

**Ultra-low Pt decorated NiCu Bimetallic Alloys Nanoparticles Supported on Reduced Graphene Oxide for Electro-oxidation of Methanol**

Ammar Bin Yousaf\*, Sajeda Adnan Mutlaq Alsaydeh, Fathima Sifani Zavahir, Peter Kasak and Syed Javaid Zaidi\*

Center for Advanced Materials, Qatar University, Doha 2713, Qatar

Corresponding Authors E-mails: [ammar.chemist18@gmail.com](mailto:ammar.chemist18@gmail.com) , [ammar@mail.ustc.edu.cn](mailto:ammar@mail.ustc.edu.cn) , [muhammad.ammar@qu.edu.qa](mailto:muhammad.ammar@qu.edu.qa) (A.B. Yousaf), [szaidi@qu.edu.qa](mailto:szaidi@qu.edu.qa) (S.J. Zaidi)


**Synthesis of graphene oxide:** The graphene oxide (GO) was prepared by the modified Hummers and Offenmans method. [1] In a typical experiment, 2 g of blank graphite powder was first added into 100 mL concentrated H2SO4 at room temperature. Under stirring, the mixture was cooled to 5 oC using an ice bath, and the temperature of the mixture was kept below 5 oC for 30 minutes. 8 g KMnO4 was then added gradually under stirring and cooling, maintaining the temperature below 10 oC. 100 mL distilled water was added into the mixture, stirred for 1 h, and further diluted to approximately 300 mL with distilled water. After that, 20 mL of 30% H2O2 was added to the mixture to reduce the residual KMnO4. The solid was filtered, washed with 5% HCl aqueous solution to remove metal ions and afterwards with distilled water until the pH was 6. The resulting graphene oxide was dried at 50 oC for 24 h.

**Reference**

1. W.S. Hummers, R.E. Offeman, Preparation of Graphitic Oxide. *J. Am. Chem. Soc.* 80, 1339 (1958).

**Table S1:** ICP-MS results for real Pt, Ni and Cu loading measurements of all the catalysts included in present study

|  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **No.** | **Catalyst** | **ICP-MS measurements** | | | | | | | | | | |
| **Pt**  **(mol)** | **Ni**  **(mol)** | **Cu**  **(mol)** | **Pt**  **(wt%)** | | **Ni**  **(wt%)** | **Cu**  **(wt%)** | **Pt**  **(wt%)** | | **Ni**  **(wt%)** | **Cu**  **(wt%)** |
| **“Actual Loadings”** | | | | **“Nominal Loadings”** | | | |
| 1 | Pt-Ni1Cu3/rGO | 2.185×10-6 | 0.002×10-3 | 0.0168×10-3 | 1.93 | 59.4 | | 18.9 | 2 | 20 | | 60 |
| 2 | Pt-Ni1Cu1/rGO | 2.211×10-6 | 0.005×10-3 | 0.0145×10-3 | 1.96 | 38.9 | | 39.3 | 2 | 40 | | 40 |
| 3 | Pt-Ni3Cu1/rGO | 2.204×10-6 | 0.008×10-3 | 0.0119×10-3 | 1.98 | 19.7 | | 58.8 | 2 | 60 | | 20 |



**Figure S1:** Electrochemical CV results taken in presence and absence of Pt loading in 0.1M KOH + 1 M CH3OH, for the analysis of electrocatalytic MOR performance of Ni1Cu3/rGO and Pt-Ni1Cu3/rGO catalysts.