**SUPPLEMENTARY MATERIAL**

**Quantitative Composition Determination by Mössbauer Spectroscopy**

B. Scotta, C.A.M. Browna, R.A. Dunlapb, and M.N. Obrovac\*a,b,c

aDepartment of Chemistry, Dalhousie University, Halifax, Nova Scotia B3H 4R2, Canada

bDepartment of Physics and Atmospheric Science, Dalhousie University, Halifax, Nova Scotia B3H 4R2, Canada

cClean Technologies Research Institute, Dalhousie University, Halifax, Nova Scotia B3H 4R2 Canada

\* - corresponding author: mnobrovac@dal.ca

**Table S1**

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  |  | Fe-content (μmoles) | |
|  | Sample (g) | Fe2O3 (g) | Sample | Fe2O3 |
| IC 0.5% Fe | 0.29743 | 0.00215 | 27.0 | 26.9 |
| IC 1.0% Fe | 0.29602 | 0.00478 | 52.8 | 59.8 |
| IC 2.0% Fe | 0.29333 | 0.00682 | 99.2 | 85.4 |
| IC 5.0% Fe | 0.29632 | 0.01984 | 266 | 248 |
| IC 10% Fe | 0.28483 | 0.02808 | 504 | 351 |
| Si 0 hr | 0.60493 | 0.02326 | 43.0 | 291 |
| Si 1 hr | 0.59966 | 0.02521 | 141 | 316 |
| Si 2 hr | 0.60136 | 0.02350 | 168 | 294 |
| Si 4 hr | 0.59724 | 0.02352 | 211 | 294 |
| Si 8 hr | 0.59362 | 0.02646 | 230 | 331 |
| Si 16 hr | 0.60101 | 0.02354 | 234 | 295 |

**Table S1** Mass of sample and Fe2O3 IS powders in all Bellcore plastic films used for quantitative Fe content determination

**Table S2**

|  |  |  |  |
| --- | --- | --- | --- |
|  | IC | Fe2O3 | FeSi2 |
| CS (mm/s) | 0.4241 | 0.3857 | 0.1443 |
| QS (mm/s) | 0.6112 | -0.1064 | 0.5587 |
| HWHM (mm/s) | 0.4754 | 0.3195 | 0.4823 |
| H (T) |  | 51.52 |  |

**Table S2** Mössbauer fitting parameters for the pure phases of the Fe containing species evaluated in this work, where H is the hyperfine magnetic field in Tesla units.