(Supplementary material)
The structure and mechanical properties of Cu50Ni50 
alloy nano-foams formed via polymeric templating

Chang-Eun Kima,b, Raheleh M. Rahimia and David F. Bahra,*

aSchool of Materials Engineering, Purdue University, West Lafayette, IN 47906-2045, USA

bLawrence Livermore National Laboratory 7000 East Avenue, Livermore, CA 94550, USA

Address all correspondence to David Bahr at dfbahr@purdue.edu

Table S1: Measured interlayer spacings from the selected area diffraction, d, with respect to various hkl, as compared to reference interlayer spacings of the bulk Cu and Ni. [1,2] The Δd values are calculated by (d-dref)/dref. The inter-layer spacing distances, d, of the Cu-Ni alloy nano-foam is in general smaller than those of Cu bulk, and larger than those of Ni bulk.

| d (Å) | dCu-bulk (Å) | ΔdCu(%) | dNi-bulk (Å) | ΔdNi(%) | (hkl) |
| --- | --- | --- | --- | --- | --- |
| 2.066 (± 0.21) | 2.088 | −1.08 | 2.034 | +1.45 | 111 |
| 1.787 (± 0.06) | 1.808 | −1.15 | 1.763 | +1.37 | 200 |
| 1.272 (± 0.03) | 1.278 | −0.46 | 1.246 | +2.09 | 220 |
| 1.080 (± 0.05) | 1.090 | −0.88 | 1.063 | +1.66 | 311 |
| 0.825 (± 0.01) | 0.829 | −0.50 | 0.808 | +2.05 | 331 |

[1]	H. E. Swanson, E. Tatge, and R. K. Fuyat, Standard X-ray diffraction powder patterns (US Government Printing Office, 1953).

[2]	F. W. Von Batchelder and R. F. Raeuchle, Acta Crystallogr. 7, 464 (1954).