Supplementary Materials

The Effect of Poly(dimethylsiloxane) (PDMS) Binder in a Silica-based Superhydrophobic Coating on Mechanical Properties, Surface roughness, and Wettability

Divine Sebastian, Chun-Wei Yao*

Department of Mechanical Engineering, Lamar University, Beaumont, TX, 77710, USA

*	Correspondence: cyao@lamar.edu; Tel.: +1-409-880-7008

Figure S1: Static contact angle image for a water droplet of 10 µL on coating-B

(b)

(a)

Figure S2: (a) and (b) shows the nanocomposite coating-B at different magnifications.

Table S1: Average values of indentation results for 400 indentations performed to get the mapping images

|  | Coating-A | Coating-B | Coating-C | Coating-D |
| --- | --- | --- | --- | --- |
| Reduced Elastic Modulus (GPa) | 2.66 ± 0.11 | 2.32 ± 0.20 | 1.59 ± 0.14 | 1.24 ± 0.21 |
| Hardness (GPa) | 0.20 ± 0.02 | 0.11 ± 0.02 | 0.05 ± 0.01 | 0.04 ± 0.01 |

Table S2: Surface roughness parameters along with static contact angle for the fabricated coatings

|  | Coating-A | Coating-B | Coating-C | Coating-D |
| --- | --- | --- | --- | --- |
| Average Roughness (RA), nm | 84.10 ± 2.2 | 105.97 ± 4.8 | 84.30 ± 3.3 | 52.54 ± 0.6 |
| RMS Roughness (RRMS), nm | 104.63 ± 1.9 | 132.80 ± 1.5 | 106.1 ± 3.1 | 66.72 ± 1.2 |
| Surface Skewness (RSK), nm | 0 | 0.16 | -0.20 | 0.27 |
| Kurtosis (RKU), nm | -0.32 | 0.17 | 0.29 | 0.14 |
| Static contact angle, (0) | 149 ± 1.0 | 155 ± 1.1 | 145 ± 1.7 | 114± 2.9 |