Supplementary Information

MEMS-based dual temperature control measurement method for thermoelectric properties of individual nanowires

Yan Cui 1,*, Yang Yang 2, Shuai Liu 3, Sheng Dai 1, Tie Li 2, Yuelin Wang 2,*

1Key Laboratory for Advanced Materials and Feringa Nobel Prize Scientist Joint Research Center, Institute of Fine Chemicals, School of Chemistry and Molecular Engineering, East China University of Science and Technology, Shanghai, 200237, China

2Science and Technology on Micro-system Laboratory, Shanghai Institute of Microsystem and Information Technology, Chinese Academy of Sciences, Shanghai,200050, China

3College of Science, Xi’an Shiyou University, Xi'an, Shaanxi, 710065, China

Figure S1  Loading of MEMS chip on the TEM sample holder. (a) the connection between electrode lead of the copper winding wire and electrode of the MEMS chip; (b) the electrical double tile TEM sample holder Gatan 646 as an example; (c) the complete loading process of the thermoelectric testing device on the TEM sample holder.

Figure S2  Voltage on hot side and cold side of the (a) (b) "sample testing" and (c) (d) "reference testing", respectively. The enlargement view of the red box in (a) was shown in (e), which shows the maximum noise of the voltage is no more than 10-4V.